## Slide 1
LARUCOLL
D4 VL82E UV
LARUCOLL D4 VL82E UV is a 1-component, D4-class PVAc-adhesive for non-structural wood applications.
PRODUCT SPECIFICATION | 
Active content | 50%
pH | Approx. 3,0
Color of the dry glueline | Transparent colorless or light colored depending on the properties of the wood product
Viscosity | 2500 - 4500 mPas (Brookfield, RV5, 20 rpm, 25°C)
STORAGE TIME AND CONDITIONS | 
In unopened containers shelf life is approximately 4 months (20°C). LARUCOLL D4 VL82E UV is freeze-thaw stabile. NOTE: After freeze-thaw cycle the product will remain as a solid, soft material and can be liquified again only by mechanical mixing. Stir the product well before use if stored for more than 2 months from the production date. Materials in contact with the product should consist of stainless steel or, inert polymeric material (PE, PP, PA or Teflon). | Unopened containers shelf life is at least 9 months (20°C). Larucoll D4/MV34 is freeze-thaw stabile. Freezing point -30°C. NOTE: If frozen, the product has to be stirred before use. Stir the product before use if stored for more than X months. Materials in contact with the product should consist of stainless steel; or inert polymeric material, such as PE, PP, PA, and/or teflon.
AREA OF APPLICATION
LARUCOLL D4 VL82E UV is developed especially for fingerjointing of wood products, that need to resist high moisture conditions. It meets requirements of EN 204 D4 and EN 14257 / WATT’91. The product is visible in UV-light.
ADDITIONAL INFORMATION
The information given in this product data sheet is based on our practical knowledge. The technical data is defined in standard conditions, and variations in local conditions and processing methods can affect to the product performance and the gluing result. No liability can be accepted from incorrect use of the product or prevailing conditions, over which we have no control. Thus, we can’t be held responsible for the final result. The user of the product must ensure the product’s suitability for the intended application.
ENVIRONMENT AND SAFETY
Always wear safety gloves and goggles. Avoid unnecessary skin contact and exposure with the liquid product. Refer to material safety data sheet. Package and the dry product waste can be disposed in normal waste according to local regulations. For further information, please contact your sales presentative at Bang & Bonsomer.
Bang & Bonsomer Group Oy | Itälahdenkatu 18 A, 00210 Helsinki | Tel. +358 9 681 081 | larucoll@bangbonsomer.com
EDITION 1 / AUG. 23RD, 2022
RECOMMENDED GLUING CONDITIONS | 
Wood moisture | 9-13%
Relative air humidity | 50% +/-5%
Temperature | 15-25°C
RECOMMENDED PRESSING CONDITIONS FOR FINGER JOINTING | 
Pressing time | Minimum time to be tested separately for each case, typically ~5 s
Typical pressure | 10-15 N/mm2
Typical application amount | 150 – 200 g/m2
Open time | < 3 minutes